Tab. 1 Description of the 7 experimental treatments. Each treatment refers to 80x80 cm area.

| Treatment type | Description | Treatment code |
| --- | --- | --- |
| Control | *No weeding treatment | Unweeded |
| Reference weeding techniques | * Herbicide application (glyphosate, 14.4 cm3 tree-1 at 1.25%) applied in May via backpack sprayer | Comm_HER |
|  | *Commercial black polyethylene film, anti-UV treated, 80 µ thick | Comm_PE |
|  | * Commercial green biodegradable woven biofilm | Comm_BF |
| Innovative groundcovers | * Recycled rubber based mulch, anti-UV treated, long-lasting and not requiring fixation (1.5 mm thick) | New_RUB |
|  | * Woven jute cloth treated with bio-based resin for increased lifetime, 100% biodegradable | New_JUTE |
|  | * Black new biopolymer-based frame, 100% biodegradable, fused to a black commercially available biodegradable film | New_BF |